## Slide 1: Complexity in Nanotechnology
Vassilios Constantoudis Institute of Nanoscience and Nanotechnology, NCSR Demokritos, Agia Paraskevi, Greece
Nanometrisis p.c., Agia Paraskevi, 153 41, Greece
NSC2022
1

## Slide 2
Traceable 3D nanometrology
HierARchical Multiscale NanoInterfaces for enhanced Condensation processes
H2020-FETOPEN-2016-2017
Projects
‘Carbyne Films: Synthesis of a New Class of Carbon Allotrope and Novel Applications in Sensors and Biosensors
CarbyneSense
A. Arapis
M. Chatzigeorgiou
A. Kondi
G. Papavieros
D. Nioras
E. Makarona
E. Gogolides
In collaboration with:
Plasma nanotechnology
A. Milionis
C.W. Edmond Lam
D. Poulikakos
Laboratory of Thermodynamics in
Emerging Technologies

## Slide 3
What is nanotechnology
What is complexity in materials
Why we need complexity in nanotechnology
Characterization of nanocomplexity
Conventional approaches
Symmetry-based approach and applications
Entropy-based approach and applications
Chaos-based approach and applications
Summary
Outline
Introduction
Previous work
New ideas
and applications
Summary

## Slide 4
What is nanotechnology - fundamentals
Nanotechnology: the design, manufacturing, characterization and performance of devices and systems enabled by embedded structures with at least one dimension <100nm (nanostructures)
Nanoparticles (3D nanostructures)
Nanowires - Nanopillars (2D nanostructures)
Thin films(1D nanostructures)
introduction

## Slide 5
What is nanotechnology - nanoproducts
introduction
More than 10.000 nanotechnology products
in market (https://product.statnano.com/)

## Slide 6
1st : Explosion of nanofabrication
techniques
2nd : Tremendous advances in
microscopy (resolution, modules)
A flood of images with a vast variety of nanostructure geometries
introduction
What is nanotechnology – the great enablers
500nm
1000nm

## Slide 7
Non-equilibrium statistical processes
Complex spatiotemporal structures
Complexity : hierarchical behaviour,
broken symmetries (between order and chaos),
scaling, nonlinearity, emergence, self-organization, adaptation, long-range correlations,…
Complexity in physics, chemistry, biology, ecology, city and earth science, astronomy,…
What is complexity in materials
Microscopic dynamics
(atomic, molecular processes)
Macroscopic phenomena
and material properties
mechanics
Statistical
Statistical mechanics deals with systems in thermodynamic equilibrium
What about non-equilibrium systems??
Complexity is a language of interdisciplinary concepts and methods

## Slide 8
Complexity vs randomness
What is complexity in materials

## Slide 9
Build the language to communicate with nanoworld complexity
The grand challenge : Quantify nanocomplexity inspired by complexity toolset
Why do we need complexity in nanotechnology
Nanostructures are the output of non-equilibrium processes
Nanomorphologies lie between fully order and fully randomness
Physicochemical properties of nanostructures depend strongly on their morphologies
Nanostructured surfaces
Fully ordered
Fully random

## Slide 10
Surface roughness – Texture morphologies
Nanoparticle metrology – Discrete structures
Fractal Approach – Scaling hypothesis
Limited fractal behavior
Non-typical roughness
No clear definition of
structures
Not to be rejected BUT to be further advanced and integrated !!!
Characterization of nanocomplexity: Previous approaches

## Slide 11
Characterization of nanocomplexity – novel approaches
Some new ideas based on concepts inspired by complexity science
Statistical/average symmetry and broken symmetries
Information entropy
Chaos and unstable dynamics
Complex networks
Hierarchical structures
…

## Slide 12
Implementation steps:
Detect and Quantify symmetry (translational, rotational, scaling)
2. Characterize deviations from perfect symmetry
A. Translational symmetry (periodic structures)
=
Focus on translational and scaling symmetry
Nanostructure Complexity => deviation from perfect symmetry
1st Idea : Symmetry-based Approach
B. Scaling symmetry (fractal structures)
=
V.C. et al. Micro Nano Engineering 2019

## Slide 13
Fourier transform
(Power Spectral Density, PSD)
Translational symmetry
=
How do we quantify it and deviations ?
Period λ
Disorder parameter
λ
?
Disorder parameter ωd : Inverse of the FWHM of the Power Spectral Density of nanostructured surfaces normalized to period
V.C. et al. MNE2019, D. Kotziambasis et al. PPP2010
1st Idea : A Symmetry-based Approach
Translational disorder (t-disorder) => ωd

## Slide 14
=
How do we quantify it and deviations ?
Fractal dimension DF
Multifractality δf
DF
Height-height correlation function (Variogram)
Multifractal spectrum
DF
δf
Scaling symmetry
1st Idea : A Symmetry-based Approach
Scaling disorder (s-disorder) => δf

## Slide 15
Surfaces: Metal Oxide (CuO) nanostructures from Hydrothermal Growth vs. rotation speed (rpm) and lab
A Symmetry-based Approach : Application 1
Disorder plane
Disorder plane shows the type and amount of symmetry deviations of surfaces
Reveals the disorder effects of experimental conditions
Scanning Electron Microscope images
V.C. et al. Micro Nano Engineering 2022

## Slide 16
A Symmetry-based Approach : Application 2
Surface disorder and preferential capture of cancer cells
Surfaces: PMMA plates after oxygen plasma etching for various times
Etching time
A. Kanioura, V.C. et al. Colloids
and Surfaces B: Biointerfaces 2019
More surface disorder =>
more preferential capture of
cancer cells

## Slide 17
Symmetry-based Approach : Limitations
The disorder parameters monotonically increase with randomness => not proper metric of complexity
Need for a quantity with minima at both full order/homogeneity and randomness and maximum in between
Symmetry/
homogeneity
randomness
complexity
Entropy S

## Slide 18
Complexity => amount of deviation from average/statistical symmetry
Complexity => maximum information => entropy-based metrics
Quantify nanocomplexity through entropy-based metrics characterizing deviation from average symmetry
From exact to average symmetry
Nanostructured surfaces as complex systems with information content
R. Alamino J. Phys. A 2015, 2017
2nd Idea : An Entropy-based Approach

## Slide 19
Implementation in 3 steps :
1st step: Calculate the local averages and generate the “mass” field m(x,y) at each scale r
2nd step: At each scale r, quantify the field homogeneity/hetetogeneity (information content) through the entropy E(r) of the normalized mass distributions λ(m|r)
r
r
3rd step: Average over all scale entropies and get the complexity (AC) of the surface
E
AC = < E(r) >r
2nd Idea : An Entropy-based Approach
Mass fields for increasing r

## Slide 20
2nd Idea : An Entropy-based Approach
Entropy
Scale r
periodic
random
Minimum complexity
complex
Maximum complexity
Complexity as average over multiscale entropy has been designed to exhibit maximum between full symmetry (homogeneity) and full randomness

## Slide 21
Entropy-based Approach - Applications
maximum
homogeneity
randomness

## Slide 22
Entropy-based Approach - Applications
Correlation length (nm)
complexity
maximum

## Slide 23
Entropy-based Approach - Applications

## Slide 24
1.
Entropy-based Approach - Applications

## Slide 25
2. Al surfaces after wet etching and boiling in CuCl2 or FeCl3
Etching with CuCl2
Etching with FeCl3
Higher complexity => larger heat transfer coefficient
Entropy-based Approach - Applications

## Slide 26
Chaos : sensitivity to initial conditions
Microscopy imaging: magnification
Idea : Use of chaos as a “dynamical microscope” of spatial complexity
3rd Idea : A Chaos-based Approach

## Slide 27
High frequencies enhancement
Increase of discontinuities
Invertible
Area preserving
Ergodic
Mixing
…
Chaos : Stretching and folding of trajectories in phase space => sensitivity to initial conditions in bound systems
3rd Idea : A Chaos-based Approach

## Slide 28
chaos
stretching
High frequencies
folding
discontinuities
Distance from randomness
Distance from uniformity
Spatial complexity
The key idea
How?
Quantification through Fourier analysis
3rd Idea : A Chaos-based Approach

## Slide 29
Chaos-based complexity measure
3rd Idea : A Chaos-based Approach

## Slide 30
  Explanation and Validation
Folding =>
discontinuities
Stretching =>
randomization
3rd Idea : A Chaos-based Approach

## Slide 31
SDb vs. correlation length and roughness exponent
  Simulated surfaces/images
Computer generated rough self-affine surfaces with controlled correlation length and roughness exponent a(=1-Fractal Dimension)
SDb is maximized at ξ=50 pix and α tending to 1
smoothness
randomness
Strong fractality

## Slide 32
  Experimental surfaces/images
Top-down SEM images of aluminum etched in hydrochloric acid for different durations a) 5 minutes in HCl, Magnitude x2000, SEI sensor b) 7 minutes in HCl, Magnitude x2000, LEI sensor c) 8 minutes HCl Magnitude x2000, LEI sensor d) 15 minutes in HCl, Magnitude x2000, LEI sensor.
5 min
7 min
8 min
15 min
SDb is maximized at t=8min
Maximization of water condensation

## Slide 33: Conclusions
Most nanosurfaces exhibit complex morphologies between order and randomness
Current approaches do not provide a concise framework for the characterization of nanocomplexity
Basic idea: Inspiration from complexity science methods
Proposal 1: A symmetry-based approach characterizes nanocomplexity with the deviation from perfect symmetry (translational => disorder parameter, scaling => multifractality)
Proposal 2: An entropy-based approach quantifies surface complexity as the average over multiscale entropy
Proposal 3: A chaos-based approach uses chaotic mixing to characterize nanocomplexity
Applications in synthesized and real data shown promising results
Higher surface disorder seems to link to more preferential capture of cancer cells
Higher entropy and chaos-based complexity leads to larger heat transfer coefficient and water condensation
Future work 1: Further understanding of the relationship of three approaches and their areas of applications
Future work 2: More theoretical and experimental investigation of the links of nanocomplexity with
fabrication parameters and surface properties

## Slide 34
Thank you very much!!!
Thank you very much!
v.constantoudis@inn.demokritos.gr